COMPDYN 2009

ECCOMAS Thematic Conference on

Computational Methods in Structural Dynamics and Earthquake Engineering

M. Papadrakakis, N.D. Lagaros, M. Fragiadakis (eds.)

Rhodes, Greece, 22–24 June 2009

fatigue lifetime estimation in structures using ambient vibration measurements

Costas Papadimitriou1, Claus-Peter Fritzen2, Peter Kraemer2, and Evangelos Ntotsios1

1University of Thessaly 
Department of Mechanical Engineering, Volos 38334, Greece
e-mail: {costasp,entotsio}@uth.gr

2University of Siegen
Institute of Mechanics and Control Engineering, Siegen 57076, Germany
{fritzen,kraemer}@imr.mb.uni-siegen.de

Keywords: Stochastic Fatigue, Damage Accumulation, Prognosis, Kalman Filter, Stochastic Dynamics, Spectral Methods.

Abstract. A methodology is proposed for estimating damage accumulation due to fatigue in the entire body of a metallic structure using output-only vibration measurements from a sensor network installed at a limited number of structural locations. This method can also be seen as a tool  for a life-time prognosis within SHM concepts. Available frequency domain stochastic fatigue methods based on Miner’s damage rule, S-N fatigue cycle curves and Dirlik’s probability distribution of the stress range are used to predict the expected fatigue accumulation of the structure in terms of the power spectral density of the stress processes. In predicting the damage and fatigue lifetime, it is assumed that the unmeasured excitations can be modeled by stationary stochastic processes. The power spectral densities of stresses at unmeasured locations are estimated from the response time history measurements available at the limited measured locations using Kalman filter and a model of the structure. The proposed formulation is demonstrated using a MDOF spring-mass chain model arising from structures that consist of members with uni-axial stress states.

INTRODUCTION

Damage accumulation due to fatigue is an important safety-related issue in metallic structures. The linear damage accumulation law introduced by [1] is often used to evaluate fatigue damage using available methods for cycle counting per stress level in measured stress response time histories. Available S-N fatigue curves [2] are used to predict the fatigue damage at different stress levels for harmonic stress time histories. The damage accumulation predictions are based on measurements taken from a sensor network, consisting usually of strain rosettes, attached to the structure and are only applicable for the locations where measurements are available. Due to practical and economical considerations, the number of sensors placed in a structure during operation is very limited and in most cases they do not cover all critical locations. Moreover, there are locations in the structure that one cannot install sensors such as underwater locations in offshore structures (oil refinery structures, offshore wind turbines, offshore steel jackets, etc.), within the body of solid structures, and non-approachable areas of extended structures. Available fatigue prediction methods based only on measurements cannot be used to predict fatigue damage accumulation at the locations where measurements are not available. In order to infer damage due to fatigue at structural members where measurements are not available, one needs to predict the stress response time histories in these structural members using the available measurements obtained from the sensory system. In limited circumstances, such predictions can be possible if one combines the available measurements with the information obtained from a model (e.g. a finite element model) of the structure.

The methods for fatigue damage accumulation have been extended to treat the case the excitations can be represented by a stochastic vector process with known correlation characteristics. Assuming that the structure behaves linearly and the excitation is modeled by a Gaussian stochastic vector process, the stress response at any point is a stochastic process that can be completely defined using the correlation characteristics of the stochastic excitations [3]. The fatigue damage accumulation at a structural location can then be computed using the characteristics of the stochastic processes of the components of the stress sensor at such location. Methods for fatigue accumulation for Gaussian narrow band stress processes have been first introduced (e.g. [4]) and then extended to the case of wide-band Gaussian stress processes (e.g. [5]). A review and comparison of spectral methods for stochastic fatigue analysis based on wide-band Gaussian stochastic processes can be found in the work by Benasciutti and Tovo [6]. The formulations depend on the probability distribution of stress cycles corresponding to different stress levels in a stress response time history signal and the expected number of peaks per unit time of a stress process. Results for the expected fatigue damage accumulation predicted by the Miner linear rule have been presented in terms of the spectral moments of the stress process which are readily obtained from the power spectral density of the stress components involved. For the important case of wide band processes encountered often in applications, simulation-inspired Dirlik approximation [5] is widely used and is considered to be the most accurate formula for modeling the probability of stress cycles in terms of the spectral moments of the stress process. It is worth noting that the aforementioned frequency domain methods based the power spectral densities use no information available from a sensor network. Instead, their predictive accuracy depend on the assumptions employed for the stochastic excitation characteristics and the models representing structural behavior. However, these prediction fail to integrate the information provided by a network of sensors. Such sensor information is expected to update and improve the fatigue predictions, making them consistent with the available measurements.

This work addresses the problem of estimating the expected damage accumulation due to fatigue in the entire body of a structure using output-only vibration measurements at a limited number of locations provided by a sensor network installed in the structure. The measurements may consist of response time histories such as e.g. strain, acceleration, velocity, displacement, etc. The proposed methodology is applicable for the case where the responses can be modeled by stationary processes and the measured response time histories are long enough so that they can be considered to approach stationary processes. The excitation in the structure is considered to be unknown. However, for most operational condition of structures for which the measured response is approaching a stationary process, the excitation can be considered to be a Gaussian stationary stochastic process with unknown intensity and frequency content.

The expected fatigue damage accumulation in the entire structure is obtained by integrating (a) methods for predicting strain/stress response time histories and their correlation/spectral characteristics in the entire structure from output-only measured response time histories available at limited locations in the structure, and (b) frequency domain methods for estimating fatigue damage accumulation using the spectral characteristics of the predicted strain/stress response time histories. The idea is to use prediction methods such as Kalman filter [7] methods to predict the strain/stress response time histories at various locations within structural components using the measurements available at a limited number of locations. Such predictions are restricted here to the case of excitations that can be adequately represented by Gaussian stationary stochastic processes.

This work is organized as follows. In Section 2, the frequency domain formulation for predicting damage due to fatigue in structural elements subjected to uniaxial stress state in linear structures under Gaussian stochastic excitations is reviewed. The formulation is applicable to Gaussian wide-band stress processes, often encountered in engineering applications, and it depends on the spectral moments of the power spectral densities of the stress process at the location of a structure. Section 3 presents the formulation for predicting the strain/stress response time histories and the associated power spectral densities at the corresponding locations of the structure using Kalman filter and the measured time histories at a limited number of locations in the structure. Section 4 demonstrates the effectiveness of the proposed methodology using a chain-like mass-spring MDOF structure and measured data that are simulated using white noise excitations. Conclusions are summarized in Section 5.

spectral method for Fatigue estimation

The Miner rule [1] is used to predict the damage accumulation due to fatigue.  According to this rule, a linear damage accumulation law at a point in the structure is defined by the formula

where  is the number of cycles at a stress level ,  is the number of cycles required for failure at a stress level , and  is the number of stress levels identified in a stress time history.  Available S-N fatigue curves [2] are used to describe the number of cycles  required for failure given a stress level . The number of cycles  at a stress level  are usually obtained using available stress cycle count methods, provided that the stress time histories are available through measurements. Alternatively, frequency domain methods based on spectral methods can be used to predict the expected damage due to fatigue using the linear damage law . The methodology assumes that the power spectral density of the stress process is available. For linear systems excited by time-varying loads that can be modeled by stationary stochastic processes, these power spectral densities can be straightforward computed using available random vibration results [3].

The methodology for estimating the fatigue accumulation at a point assuming a uni-axial stochastic stress state is next reviewed. For multi-axial stress states one can refer to the work by You and Lee [8] and Pitoiset and Preumont [9] to extend the applicability of the present methodology. Let  be the uni-axial stress at a point in a structural element. The stress is considered to be a stationary Gaussian stochastic process. This is the case encountered in linear structures that are subjected to stationary Gaussian stochastic processes. Let  be the power spectral density of the stationary Gaussian stochastic process  and

be the spectral moments of the stress process. Using frequency domain methods for fatigue estimation under stochastic excitations and the linear damage accumulation law  , the expected fatigue damage accumulation for a uni-axial stochastic stress process is given by [6]

where  is the number of cycles at stress levels within the stress interval ,

is the number of cycles for failure that correspond to a specific harmonic stress level of amplitude  obtained from available S-N curves [2],  is the expected number of peaks per unit time for the stress process,  is the probability distribution of the stress cycles at stress levels within , and  the period of observation. The parameters  and  are constants obtained from fatigue test experiments and depend on the material of the test specimen.

The expected time of failure due to fatigue (fatigue lifetime)  corresponds to a critical expected damage value  which is often set equal to unity (). Using , the fatigue lifetime is given by

where  is the expected damage rate given by

For Gaussian stochastic stress processes, the probability distribution of the stress cycles at stress levels within  is given by the Dirlik formula [5,10-11] as

where

is the range of the stress process, and , , ,  and  are specific algebraic functions of the spectral moments , , , , given by

This is a semi-empirical probability density which is a mixture of one exponential and two Rayleigh distributions. It has been derived by fitting the shape of a rain-flow range distribution via minimizing the normalized error between the rain-flow ranges and the above density model. The spectral moments  constitute a base for the construction of the approximate closed-form Dirlik formula for the probability density of the stress range. The Dirlik formula constitutes an extension of the Rayleigh distribution to non-narrow band processes. It is widely used for fatigue crack estimation under wide-band Gaussian stationary applied stress. Extension to non-Gaussian stress processes requiring the skewness and kurtosis of the stress process are available in the work by [12].

Using results from random vibration theory, the expected number of cycles  per second for a stochastic process is given by the spectral moments of the process in the form

Substituting  into  and using the fact that , one obtains the expected damage rate in the form

Using the Dirlik formula  and carrying out the integration analytically, the expected damage rate simplifies to [6]

It is clear from the aforementioned formulation and equations  and  that the expected fatigue damage rate and, consequently, the fatigue accumulation during a time interval  at a point in the structure depends only on the spectral moments , , of the stress process . Using the definition of the spectral moments in , the spectral moments and the fatigue predictions at a point of a structure eventually depend only on the power spectral density  of the stress process . The power spectral densities of the stress response processes at a point can be calculated from measurements, provided that these measurements are long enough to be considered stationary.

However, there is a limited number of points that can be instrumented in the structure. For the points where measurements are not available, one has to make predictions of the stress process and subsequently the power spectral density of the stress process, given the measurements at other locations. This issue is addressed at the next section. Once these measurements and predictions of the stresses are estimated at measured and unmeasured locations, the power spectral densities and the corresponding damage accumulation due to fatigue are obtained, using  and , everywhere in the structure. In this way, fatigue damage accumulation maps for the entire structure are constructed from limited number of vibration measurements.

REsponse predictions in the entire structure using vibration measurements

The objective of this section is to predict the stress response at all points (or DOFs) in a structure using the measurements at a limited number of locations (or DOFs). This is achieved using Kalman filter [7]. For convenience and without loss of generality, it is assumed in the analysis that sensors that are placed in the structure measure the strains.

Consider the dynamic response of a linear structural system subjected to deterministic and random excitations. Using a spatial discretization method, such as finite element analysis, the equations of motion for a linear structure are given by the following set of  second order differential equations

where  is the displacement vector, ,  and  are respectively the mass, damping and stiffness matrices,  and  are the deterministic and stochastic excitation vectors applied respectively at  and  DOFs, and  and  are matrices comprised of zeros and ones that maps the  and  excited DOFs to the  output DOFs. Throughout the analysis, it is assumed that the system matrices ,  and  are symmetric. Let  be the vector that collects all measurements at different locations of the structure at time . These measurements are collected in general from sensors such as accelerometers, strain gauges, etc.

Introducing the state vector

the equation of motion can be written in the state space form

the measured output vector  is given by the observation equation

where ,  and  are the state transition and observation matrices given by

respectively.

Kalman filter approach

Since measurements are available in digitized form, the presentation of the Kalman filter is next given in discrete time. Using the sampling rate , the discrete-time state space model corresponding to  and  is

where  and , , are the digitized state and output vectors, and

is the state transition matrix for the discrete formulation. The random variables  and  represent the stochastic excitation and the measurement noise, respectively. They are assumed to be independent, white and following normal probability distributions  and , where  and  are the stochastic excitation and the measurement noise covariances assumed to be constant, independent of time.

Kalman filter is used to estimate the state  of the system described by  using the measurements in the vector  in . Specifically, in the prediction step, an apriori state estimate  of the state vector  of the system is estimated from equation [7]

In the correction step, the measured value  is used to calculate an a posteriori state estimate , weighting the measured and estimated signals by the Kalman filter gain matrix . This is formulated by the equation

where the Kalman gain factor is given by

and, for steady state response, the error covariance matrix , where  is the a priori error estimate, satisfies the discrete time Riccati equation:

Let  be a vector containing the digitized stresses at various locations of the structure. Using structural mechanics theory, these stresses in the vector  are related to the state vector through a linear transformation , where  is the transformation matrix that associates the state vector to the desired stresses in the entire structure. Consequently, an estimate of the stresses  at time  is related to the state vector estimate  through the transformation:

Herein, the response prediction vector  is restricted to stresses at elements subjected to uni-axial stress states required in lifetime fatigue estimation as described in Section 2.

Using the definition of the cross power spectral density and the Kalman filter equations  and , the cross power spectral density  of the stress response vector  is given with respect to the cross power spectral density  of the measurement vector  in the form

where  is the matrix given by

and  is the identity matrix. Equation  relates the power spectral densities of the stresses at various structural locations with the power spectral densities of the measured quantities in  available at the limited number of measured locations. This relation depends on the model (e.g. a finite element model) used to represent the behavior of the structure and the assumption that the excitation vector is broad-band so that the excitations can be modeled by zero-mean stationary white noise processes with spectral density described by , where  is the Kronecker delta.

It should be noted that in order to apply , an estimate of the zero-lag covariance  of the unknown input stochastic process has to be provided. This estimate is obtained using the measurements  and the relation  between the covariance matrix  of the measurement vector  and the covariance matrix  of the excitation process. Using  with , this relation is given by

where  is given by the discrete time Lyapunov equation in the form

The optimal values of the entries of the covariance matrix  can be obtained by minimizing the difference between the covariance matrix  predicted by the linear model given  and the covariance matrix  obtained from the measurements in , . That is, the optimal value  is obtained by minimizing the objective function

with respect to the elements in . The optimal value  of  is then substituted in  to completely define the Riccati equation . The solution  of the Riccati equation is substituted in  in order to find  which is needed in .

Estimation of power spectral densities of stresses

The cross power spectral density matrix  of the sampled measurement vector , involved in , can be obtained using available signal processing techniques such as the Welch technique [13]. Once  has been estimated from the measurements, equation  is used to estimate the cross power spectral density  of the stress response vector . Alternatively, the PSD  of the stress response vector  is obtained by using equations  and  for the Kalman filter to provide estimates  of the system state vector which are then used in equations  to estimate the stress vector . Finally, available signal processing techniques such as the Welch technique are used to compute the PSD  from the sampled stress response vector . The length of the sampled time history should be sufficient large in order for the estimates to be accurate.

The diagonal elements  of the cross power spectral density matrix  given in  contain the power spectral density estimates required for fatigue predictions using equations  and .

Application

The applicability and effectiveness of the methodology is illustrated using simulated “measurements” from a simple spring mass chain-like model of a structure. The stress state at critical locations are uni-axial and the fatigue prediction methodology can be directly applied. The measurements are assumed to be strain measurements. These measurements are simulated from the model of the structure using wide-band excitation resembling white noise.

Consider the class of -DOF spring mass chain-like model fixed at the two ends as shown in Figure 1. The model is used to represent a structure consisting of a series of bar and body elements as shown in Figure 2. The structure consists of  bodies with the -th body having mass . The  and the  bodies are connected by elastic bar element which provide the stiffness  to the system. The number of bar (or spring) elements of the chain model is . The material of the bar elements is considered to be steel. For steel bar elements, the values of the fatigue constants in equation  are taken to be  and  for steel samples.  The -th bar element has length , cross-sectional area  and modulus of elasticity .  For simplicity, each bar element is represented by a spring element with stiffness  as shown in Figure 1. Also, the nodal mass  in Figure 1 includes the effect of the  body mass and the lumped mass arising from the bar elements connected to node . The  component  of the vector  corresponds to the displacement of the node  of the model. The system is subjected to an unmeasured excitation applied at node .

Figure 1: -DOF spring mass chain-like model.

Figure 2: Structure consisting of  masses and  bar elements.

| Property Type | Property Value | Units |
| --- | --- | --- |
| Material | Steel |  |
| Modulus of Elasticity, | 2.1e11 |  |
| Radius | 3.5e-3 |  |
| Length | 300e-3 |  |
| Stiffness | 2.7e7 |  |
| Mass | 21 |  |
| Mass | 15 |  |
| Mass | 12 |  |
| Mass | 15 |  |
| Mass | 21 |  |

Table 1: Geometric and material properties.

For demonstration purposes, the excitation vector  is assumed to be broadband and is modeled by Gaussian stationary white noise vector process with constant spectral density matrix. White noise provides a good approximation of the input whenever the correlation time of the input is sufficiently small compared to the system time constants. The discrete state space formulation of the equations of motion is used to simulated response time history data as well as compute estimates of the covariance responses and the power spectral density of the responses using the white noise excitation applied at node . In particular, the strain and stress response time histories  and , respectively, are simulated at all bar elements using the state space formulation. The time discretization step used in simulated the sampled data is  seconds. The simulated strain and stress response time histories are the reference stress response time histories that are considered to be the exact stress response time histories for the excitations used. These response time histories and the corresponding power spectral densities can be used with the fatigue prediction methodology to compute the lifetime of the structure due to fatigue failure. Such predictions constitute the reference (exact) predictions against which the predictions from the proposed Kalman filter approach should be compared to for assessing the accuracy of the proposed methodology.

Let  be the set that contains the bar element numbers where the strains are measured. The simulated sampled time history of the strain responses  associated with the nodes or DOFs included in the set  are included in the measurement vector . In practice, these measurements are collected using appropriate sensors such as strain gauges. Let  be the set that contains the bar element numbers where the stresses will be predicted. The set  is selected to be , i.e. it is assumed that stresses are predicted at all bar elements.

Results demonstrating the effectiveness of the proposed methodology are presented for a five degree of freedom system () shown in Figure 1. The nodal masses as well as the geometric and material properties of the bars are listed in Table 1. The damping matrix  in the equations of motion is chosen assuming that the system is classically damped. Rayleigh damping is assumed, i.e. . A single excitation is considered which is applied at node . The strain response time histories  at the measured DOFs are used to predict the stress response time histories at all bar elements identified in the set  using the proposed Kalman filter approach.

Figure 3: Comparison between reference and estimated from Kalman filter stress response time histories.

Comparison between the reference (exact) stress time histories simulated by the model and the estimated time histories from the Kalman filter are given in Figure 3 for all bar elements in the set , assuming that the measured strains are at bar elements . Similar comparisons for the power spectral densities of the stress time histories are shown in Figure 4. It can be seen that the estimated stress time history and the power spectral densities of the stress at the bar elements 2 and 4, where measurements are available, coincides with the corresponding reference stress time histories and stress power spectral densities simulated by the model. At the other bar elements, there is a discrepancy between the estimated and reference (exact) stress time histories or power spectral densities. These differences are due to the estimation error associated with the Kalman filter. However, it should be noted that the predictions from the Kalman filter approach are quite good, especially for the high amplitudes around the resonance peaks which mainly contribute to the fatigue process.

Figure 4: Comparison between reference and estimated from Kalman filter power spectral densities of the stress responses.

Lifetime predictions due to fatigue are shown in Figure 5 for all six bar (spring) elements of the structure as a function of the intensity  of the input white noise, where  is the standard deviation of the input. The lifetime values in the Figure are obtained using the fatigue prediction formula . For each bar element, there are two lifetime fatigue predictions. The first prediction is based on the reference time histories simulated by the model and it is used as the exact value against which to study the accuracy of the predictions from the proposed methodology. The second fatigue-based lifetime estimate is the one predicted by the methodology based on the use of Kalman filter approach to estimate the stress response time histories at all bar elements.

Figure 5: Comparison of reference fatigue-based lifetime estimates and the estimates predicted by the Kalman filter as a function of the excitation amplitude for the  DOF model.

To study the effect of the number and location of sensors (measurement points) on the accuracy of the predictions, Figures 6a and 6b presents predictions in the entire structure (all six bar elements) using two sensors placed at bar elements  and , respectively, while Figures 6c and 6d present predictions using three and four sensors placed at bar elements  and , respectively.

Figure 6: Comparison of reference fatigue-based lifetime estimates and the estimates predicted by the Kalman filter for the  DOF model.

It can be seen that the estimates based on the Kalman filter predictions are quite close to the reference fatigue values obtained from the actual simulations. Comparing the fatigue lifetime predictions in Figures 6a-d, it becomes clear that the accuracy of the predictions depend on the number and location of sensors in the structure. One can improve the estimates considerably using optimal sensor location methodologies [14].

CONCLUSIONS

A methodology for estimating damage due to fatigue on the entire body of a structure using spectral methods and output only vibration measurements at a limited number of locations was presented. The fatigue predictions presented in this work are limited to structural members subjected to a uni-axial stress state. These predictions can be extended using available methods to structural members subjected to multi-axial stress state. Kalman filter is used for predicting the power spectral densities of the stresses in the entire body of the structure using the available measurements and a model of the structure. These predictions can be used to construct fatigue accumulation and lifetime prediction maps consistent with measurements provided by a monitoring system. The results from the proposed methodology are useful for designing optimal maintenance strategies for metallic structures using information for the actual condition of a structure, collected from a sensor network placed at limited number of locations.

Acknowledgements

This research was funded by the Greek National Scholarship Foundation (IKY) within the IKYDA program framework and by the Deutscher Akademischer Austausch Dienst (DAAD, German Academic Exchange Service) within the PPP program. This research was also co-funded 75% from the European Union (European Social Fund), 25% from the Greek Ministry of Development (General Secretariat of Research and Technology) and from the private sector, in the context of measure 8.3 of the Operational Program Competitiveness (3rd Community Support Framework Program) under grant 03-ΕΔ-524 (PENED 2003).

REFERENCES

M.A. Miner, Cumulative damage in fatigue. J Appl Mech, 12, A-159, 1945.

B.F. Langer, Design of pressure vessels for low-cycle fatigue. ASME J. Basic Eng, 84, 389–402, 1962.

L.D. Lutes, S. Sarkani, Random vibrations: analysis of structural and mechanical systems. Butterworth-Heinemann, 2003.

I., Rychlik, On the ‘narrow-band’ approximation for expected fatigue damage. Probabilistic Engineering Mechanics, 8, 1–4, 1993.

T. Dirlik, Applications of computers to fatigue analysis. PhD Thesis, Warwick University, 1985.

D. Benasciutti, R. Tovo, Comparison of spectral methods for fatigue analysis of broad-band Gaussian random processes. Probabilistic Engineering Mechanics, 21, 287–299, 2006.

G.F. Franklin, J.D. Powell, M.L. Workman, Digital control of dynamic systems. Second Edition, Addison-Wesley, 1990.

B.R. You, S.B.  Lee, A critical review on multiaxial fatigue assessments of metals. International Journal of Fatigue,18 (4), 235–244, 1996.

X. Pitoiset, A. Preumont, Spectral methods for multiaxial random fatigue analysis of metallic structures. International Journal of Fatigue, 22, 541–550, 2000.

N.N. M. Bishop, F. Sherrat, A theoretical solution for the estimation of the rainflow ranges from power spectral density data. Fatigue and Fracture of Engineering Materials and Structures, 13 (4), 311-326, 1990.

D. Benasciutti, R. Tovo, Spectral methods for lifetime prediction under wide-band stationary random processes. International Journal of Fatigue, 27, 867–877, 2005.

X. Wang, J.Q. Sun, Multi-stage regression fatigue analysis of non-Gaussian stress processes. Journal of Sound and Vibration, 280, 455-465, 2005.

P.D. Welch, The use of fast Fourier transform for the estimation of power spectra: A method based on time averaging over short modified periodograms. IEEE Trans. Audio Electroacoustics, 15, 70-73, 1967.

C. Papadimitriou, Optimal sensor placement methodology for parametric identification of structural systems. Journal of Sound and Vibration, 278(4), 923-947, 2004.